| Table 4. SR, KA and MRR values for multiple experiments |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | S.no | pressure (MPa) | stand of distance (mm) | traverse speed (mm/min) | Mass flow rate (kg/min) | Surface roughness (µm) | Material removal rate (mm3/sec) | kerf |
|  | 1 | 220 | 2 | 80 | 0.4 | 4.75 | 119.98 | 2.08 |
|  | 2 | 260 | 1 | 64 | 0.55 | 3.09 | 126.36 | 1.44 |
|  | 3 | 220 | 2 | 80 | 0.45 | 4.46 | 122.4 | 1.98 |
|  | 4 | 140 | 3 | 96 | 0.55 | 5.02 | 111.57 | 2.25 |
|  | 5 | 300 | 1 | 96 | 0.35 | 3.84 | 126.63 | 1.75 |
|  | 6 | 140 | 1 | 64 | 0.35 | 5.04 | 97.63 | 2.25 |
|  | 7 | 220 | 2 | 72 | 0.45 | 4.38 | 121.6 | 1.95 |
|  | 8 | 140 | 3 | 64 | 0.55 | 4.61 | 109.81 | 2.09 |
|  | 9 | 280 | 2 | 80 | 0.45 | 4.14 | 137.08 | 1.83 |
|  | 10 | 300 | 1 | 64 | 0.35 | 3.5 | 117.28 | 1.59 |
|  | 11 | 300 | 3 | 96 | 0.35 | 3.97 | 143.3 | 1.86 |
|  | 12 | 220 | 2 | 88 | 0.45 | 4.63 | 125.7 | 2.04 |
|  | 13 | 140 | 3 | 96 | 0.35 | 5.56 | 106.95 | 2.57 |
|  | 14 | 300 | 3 | 96 | 0.55 | 3.62 | 148.41 | 1.64 |
|  | 15 | 140 | 1 | 64 | 0.55 | 4.08 | 102.02 | 1.86 |
|  | 16 | 180 | 2 | 80 | 0.45 | 4.75 | 115.2 | 2.15 |
|  | 17 | 220 | 2 | 80 | 0.45 | 4.46 | 122.4 | 1.98 |
|  | 18 | 220 | 1.5 | 80 | 0.45 | 4.41 | 119.69 | 1.96 |
|  | 19 | 300 | 3 | 64 | 0.55 | 3.42 | 145.92 | 1.52 |
|  | 20 | 220 | 2 | 80 | 0.5 | 4.27 | 131.74 | 1.93 |
|  | 21 | 220 | 2.5 | 80 | 0.45 | 4.67 | 132.71 | 2.05 |
|  | 22 | 140 | 1 | 96 | 0.35 | 5.36 | 99.7 | 2.43 |
|  | 23 | 300 | 1 | 96 | 0.55 | 3.29 | 140.98 | 1.48 |
|  | 24 | 220 | 2 | 80 | 0.45 | 4.46 | 122.4 | 1.98 |
|  | 25 | 140 | 1 | 96 | 0.55 | 4.53 | 104.26 | 2.08 |
|  | 26 | 140 | 3 | 64 | 0.35 | 5.23 | 103.66 | 2.34 |
|  | 27 | 300 | 3 | 64 | 0.35 | 3.80 | 139.85 | 1.73 |

| Output | Ridge Hyper parameter | Ridge R² | RF Hyper parameter | RF R² | XGB Hyperparameter | XGB R² | NN Hyperparameter | NN R² |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| surface Roughness | {'alpha': 1, } | 0.926 | {n_estimators=100, max_depth=10} | 0.971 | {n_estimators=100, max_depth=5, learning_rate=0.05} | 0.997 | {'hidden_layer_sizes': architecture=(6,4,3), alpha=0.001, learning_rate=0.0} | 0.925 |
| MRR | {'alpha': 1, } | 0.940 | {'n_estimators':100, 'max_depth':10} | 0.973 | {'n_estimators':100, 'max_depth':5, 'learning_rate':0.05, 'subsample':0.8} | 0.997 | {'hidden_layer_sizes:' architecture=(8,5,4), alpha=0.001, learning_rate=0.01} | 0.946 |
| Kerf Angle | {'alpha': 1, } | 0.967 | {'n_estimators':100 ,'max_depth':10} | 0.907 | {'n_estimators':100, 'max_depth':5 ,'learning_rate':0.05, 'subsample':0.8} | 0.996 | {'hidden_layer_sizes': architecture=(6,4,2), alpha=0.001, learning_rate=0.01} | 0.850 |

Table 5: Hyperparametrs for optimized models.

Fig. 5.  architecture for SR, MRR, and kerf angle models step 3: Ensemble Model Creation.

- (b)

(c)

Fig. 7. Validation of each model with experimental value

Table 6: Ensemble Model performance.

| Ensemble Model Performance Summary |  |  |  |
| --- | --- | --- | --- |
| Target | RMSE | MAE | R² |
| Surface Roughness | 0.0768 | 0.0563 | 0.9484 |
| Material Removal Rate | 2.9824 | 2.5181 | 0.9571 |
| Kerf Angle | 0.0345 | 0.0294 | 0.9845 |

SURFace roughness:

(a)                                                              (b)                                                                 (c)

Fig. 8. Ensemble Surface Roughness Model Performance (a) Training and    Validation Curve (b) Actual vs Predicted value (c) Density curve (d) Heat map.

(d)

Fig. 11. Learning curve for Cross-validation Surface Roughness

Material Removal Rate

- (b)                                                                     (c)

Fig. 8. Ensemble Material Removal Rate Model Performance (a) Training and Validation Curve (b) Actual vs Predicted value (c) Density curve (d) Heat map.

(d)

Fig. 11. Learning curve for Cross-validation Material          Removal Rate.

KERF ANGLE

(a)                                                                       (b)                                                                       (c)

Fig. 8. Ensemble Kerf Angle Performance                      (a)  Training and Validation Curve (b) Actual vs Predicted value (c) Density curve (d) Heat map.

Fig. 11. Learning curve for Cross-validation Kerf Angle

| Table 3: Optimal Process Parameter Settings for Different Objectives |  |  |  |
| --- | --- | --- | --- |
| Parameter | Min Kerf | Max MRR | Balanced |
| Pressure (MPa) | 260 | 300 | 300 |
| Standoff Distance (mm) | 1 | 3 | 3 |
| Traverse Speed (mm/min) | 64 | 96 | 96 |
| Mass Flow Rate (kg/min) | 0.55 | 0.55 | 0.55 |
| Expected Kerf (°) | 1.47 | 1.66 | 1.66 |
| Expected MRR (mm³/min) | 128.31 | 150.03 | 150.03 |

| Table 3: Optimal Process Parameter Settings for Different Objectives |  |  |  |
| --- | --- | --- | --- |
| Parameter | Min Ra | Max MRR | Balanced |
| Pressure (MPa) | 260 | 300 | 300 |
| Standoff Distance (mm) | 1 | 3 | 3 |
| Traverse Speed (mm/min) | 64 | 96 | 96 |
| Mass Flow Rate (kg/min) | 0.55 | 0.55 | 0.55 |
| Expected Ra (μm) | 3.23 | 3.65 | 3.65 |
| Expected MRR (mm³/min) | 128.31 | 150.03 | 150.03 |

| Table 3: Optimal Process Parameter Settings for Different Objectives |  |  |  |
| --- | --- | --- | --- |
| Parameter | Min Ra | Min Kerf | Balanced |
| Pressure (MPa) | 260 | 260 | 260 |
| Standoff Distance (mm) | 1 | 1 | 1 |
| Traverse Speed (mm/min) | 64 | 64 | 64 |
| Mass Flow Rate (kg/min) | 0.55 | 0.55 | 0.55 |
| Expected Ra (μm) | 3.09 | 3.09 | 3.09 |
| Expected MRR (mm³/min) | 1.47 | 1.47 | 1.47 |

Distribution:

BOOSTRAP

HYBRID Ensemble: